# Manufacturer: Jacksons Fencing

# Web: www.jacksons-security.co.uk

# Tel: +44 (0)1233 750393 | 0800 953 3699

Product Reference: EuroGuard® Flatform Heavy A1 (SR1)

Twin wire mesh fencing (868) LPS 1175 A1 certified fencing

Certification:

LPS 1175 A1 (SR1)

# Guarantee:

# Steel fencing and gates designed and manufactured to be fit for purpose and providing a minimum 25 year guarantee, delivering the lowest whole life cost and significantly reduced carbon footprint.

# Typical Fencing & Posts (Subjective to site location):

[2030mm High, post dimensions 60 x 40mm]

[2430mm High, post dimensions 80 x60mm]

# Mesh:

200 x 50mm mesh, double 8mm horizontal wire, 6mm vertical wire.

# Panel Construction:

[Heavy double 8mm wire]

Mesh panels with flat profile with double horizontal wires with 192 x 44mm apertures, welded at intersections.

# Fixings:

Fence panels are fixed to posts with matching Jacksons proprietary vandal-proof panel fixings

# Finish / Colour:

Galfan® zinc alloy coated to BS EN 10244-2:2009 class A. Posts supplied galvanised inside and out to BS EN 1461 as standard.

Galvanised  to BS EN 1461then polyester powder coated with architectural grade Akzo Nobel Interpon powder in standard  [Black RAL 9005]. [Green RAL 6005].  [White RAL 9010]. [Blue RAL 5010]. [Blue BS 20-C-40]. [Brown RAL 8017]. [Yellow RAL 1018]. [Grey RAL 7012]. [Red RAL 3020]. Or special [Insert RAL/BS].

# Installation:

# Set out and erect:

- Alignment: Straight lines or smoothly flowing curves, fence line may be stepped to accommodate sloping or uneven ground.

- Tops of posts: Following profile of the ground.

- Setting posts: Rigid, plumb and to specified depth, or greater where necessary to ensure adequate support.

- Fixings: All components securely fixed.

# Setting posts in concrete:

- Standard: To BS 8500-2.

- [Mix: Designated concrete not less than GEN1 or Standard prescribed concrete not less than ST2.]

- [Alternative mix for small quantities: 50kg Portland cement to150kg fine aggregate to 250kg, 20mm nominal maximum size coarse aggregate, medium workability.]

- [Admixtures: Do not use].

# Holes: Excavate neatly and with vertical sides, with a size appropriate to the site exposure and local ground.

- Filling: Position post/strut and fill hole with concrete to not less than the specified depth, well rammed as filling proceeds and consolidated.

- [Backfilling of holes not completely filled with concrete: Excavated material, well rammed and consolidated.

# Completion:

# Cleaning:

- General: Leave the works in a clean, tidy condition.

- Surfaces: Clean immediately before handover.

# Fixings:

- All components: Tighten.

- Timing: Before handover.

NOTES:

For more information please contact Jacksons Fencing. We reserve the right to alter specification within this document at any time.